L3 Land-based Service Engineering - Task Sheet

NAME:.....................................................................................	DATE:................

Reference:	Task:

305/04	ID WELDING DEFECTS

Requirements:

Selection of different welds either your samples or actual

Guide notes.

Instructions:

Critically examine each of the welds for defects.  In the table over describe their appearance and a possible cause.

Note:  it is not essential that all six rows are completed.

(An Activity Sheet will not be required for this task)

Method:

- Examine closely the weld beads for faults.

2.	With the help of the supplied guide notes, identify the defect and suggest a possible cause on the proforma over.

TASK COMPLETE

Signed (Trainee):..........................................................	Date:...............................

Signed (Assessor):.......................................................	Date:...............................

over/

| Item No. | Sample: ( | Defect: | Cause: | Correctly identified? |
| --- | --- | --- | --- | --- |
| 1 | MMA ( MAGS ( TIG ( | Butt ( Fillet ( Lap ( |  |  |  |
| 2 | MMA ( MAGS ( TIG ( | Butt ( Fillet ( Lap ( |  |  |  |
| 3 | MMA ( MAGS ( TIG ( | Butt ( Fillet ( Lap ( |  |  |  |
| 4 | MMA ( MAGS ( TIG ( | Butt ( Fillet ( Lap ( |  |  |  |
| 5 | MMA ( MAGS ( TIG ( | Butt ( Fillet ( Lap ( |  |  |  |
| 6 | MMA ( MAGS ( TIG ( | Butt ( Fillet ( Lap ( |  |  |  |